## Slide 1: Electric Machine Design Course
Magnetic Materials for Electric Machines
Lecture # 9

## Slide 2: Active magnetic materials used in electrical machines
All electric machine types require soft pure iron materials to carry magnetic flux around the circuit.
Impurities like carbon contribute to hysteresis losses
Hi-flux densities & frequencies contribute to eddy current losses
Permanent magnets are considered hard materials
Best grades exhibit high hysteresis residual flux
All electric machines require conductors of electricity
Copper has lowest electrical resistance
Aluminum is a good choice for cast cage rotors

## Slide 3: Two magnetic material classes
Soft materials: Small hysteresis
Electrical steels
Pure iron bar stock
Sintered pure iron
Hard materials: Large hysteresis
Permanent Magnets
2.1 Tesla
1.4 Tesla

## Slide 4: Electrical steels (soft iron)
Rotor & stator cores from sintered electrical steel grades
Can be used for complicated core shapes
Rotor & stator core laminations punched from electrical steel lamination grades with low cope loss & surface insulation.
Non-Oriented Silicon M-19 grades # 24, # 26 & # 29 gages
Oriented M-3 grades (0.003” thick)
Stator core components from Amorphous materials (MetGlas)
Lowest core losses with fabrication difficulties
Medium to low flux densities (1.56 T max)
Both Fe & Co based alloys available

## Slide 5: TITLE
Soft Sintered Magnetic Materials

## Slide 6: Powdered soft iron magnetic components
SOLALOY iron coated magnetic powders with
an insulating layer and compacted into complex shapes used for electric motor stator & rotor
components .

## Slide 7: ASTM vs. EN/IEC gages & core losses

## Slide 8: Electrical steel grades for laminated cores

## Slide 9: Misleading B-H plots for electrical steels

## Slide 10: Low loss electric steels for medium to high frequency machines
Frequency = rpm x 2p / 60

## Slide 11: Lamination coatings to insulate against eddy current losses

## Slide 12: TITLE
METGLAS
Soft Iron
lowest core loss materials
Very thin & difficult to punch for
motor cores

## Slide 13: Losses in electrical steels
Iron loss: losses generated in the iron core parts
such as stator yoke and stator teeth are caused by changing magnetic fields.
Total iron losses are composed of two loss components:
Hysteresis losses
Eddy current losses

## Slide 14
Calculation of Hysteresis Loss (Watts)
by analytical means or FEA
Modeling methods such from Preisach, Hysteron & Curling are used for hysteresis loss calculations or predictions
Hysteresis losses are equal to area inside
of the B-H loop charted when material is
subjected to magnetization to saturation
and complete de-magnetization
Hysteresis Losses::
f = frequency
t = lam thickness
σ = lam conductivity
ρ = density
M= Mass of core
C = Steinmetz
hysteresis
coefficient

## Slide 15: Calculation of Eddy Current Loss (Watts) by analytical means or FEA
Eddy Current Losses:
Calculate sum of each part of the stator lamination
Multiply by watts/Kg and sum losses.
Note: might be different in lamination sections
such as stator vs rotor or yoke & teeth
f = frequency
t = lam thickness
σ = lam conductivity
ρ = density
M= Mass of core
C = Steinmetz
hysteresis
coefficient

## Slide 16: Separation of Hysteresis & Eddy Current Losses

## Slide 17: Radial or parallel orientation & magnetization
Approximate same flux from both magnets !

## Slide 18
Permanent Magnetic Comparisons
/4800
/550
NdFeB Grades
All current magnet
grade categories
/4460
/5.5

## Slide 19: Permanent magnet grades
Magnequench

## Slide 20: High flux ceramic magnet (TDK FB12B)

## Slide 21: Permanent Magnet Summary

## Slide 22: Low cost magnet material comparison

## Slide 23: Neodymium Boron Iron magnet grades

## Slide 24: Samarium Cobalt grades

## Slide 25: Samarium Cobalt, B-H data vs. temperature

## Slide 26: Samarium Cobalt B-H data (550 deg C)

## Slide 27: Load line of magnet with air-gap & de-mag plot
NdFeB magnet data
Load line
1.1 T = Bg
@
Plot load line & project to Bm and read Bg
Move load line to intrinsic curve knee, Read (– H) value @ *
and convert to peak de-mag phase amps.
Read 7 kOe converts
to 557,042 NI/M
Divide by the magnet path length and the number of turns and the result is the min de-mag current
*

## Slide 28: Normal & Intrinsic B-H curves
MMPA
Second quadrant is the de-magnetization curve
The normal curve plot frequently does not show the “knee” of the curve as it appears in the third quadrant
The Intrinsic plot of the same data moves the knee into the second quadrant where the load line can be placed right before the slop of the curve begins to change.
For each –H value, positive value of –H is added to the corresponding B value for the intrinsic plot.

## Slide 29: De-magnetization study
-H max
Pc = Lm/Lg
= (Load line)
-H max for zero
de-magnetization

## Slide 30: TITLE

## Slide 31: TITLE